## Slide 1: Presentation in Conference on
Exploring Innovative Research Methodologies in a Variety of Multidisciplinary Fields and Their Prospective Future Impact
Presentation Topic
Synthesis of MnO2 Nanostructure by SILAR Technique

## Slide 2: Presented by Mahesh Kumar
Research Scholar
Mangalayatan University Aligarh

## Slide 3: Supervisor - Prof. Yatendra Pal Singh HOD Physics Department Mangalayatan University, Aligarh Co Supervisor - Prof. (Dr.) Vaibhav Jain Principal C. L. Jain (PG) College, Firozabad

## Slide 4: Abstract
Numerous in-depth studies have been conducted on manganese oxide nanoparticle, which has led to the discovery of their applicability in a variety of fields
Because of the wide variety of catalytic and adsorptive qualities it exhibits, particles composed of manganese oxide (MnO2) have lately attracted a lot of interest in the scientific community
MnO2 has emerged as the most promising metal oxide. MnO2 is a versatile material that can take on a variety of different forms, or polymorphs, and each of these forms has its own set of features

## Slide 5: The SILAR method's benefits include a large area deposition, which could be carried out in any substrate at lower temperatures by using simple techniques and inexpensive instruments; stoichiometry, thickness, morphology, and grain size could be controlled The SILAR deposition was accomplished by performing a series of 10-second immersions on a cleaned FTO-coated glass substrate in aqueous solutions containing 0.09 M MnSO4 and (0.1M) hydrazine hydrate the substrate was washed for ten seconds in double-distilled water to eliminate species that were only lightly adsorbed

## Slide 6: In scanning electron micrographs of MnO2 thin films we can see plainly discern compact coverage throughout the entirety of the substrate The capability of our synthesis process leads to the development of films with minimal thickness, high compactness, and quality adhesion, all of which are likely explanations for high specific capacitance in comparison to prior reports The electrochemical phase transition happens when Na+ ions are inserted into the crystal structure of Mn3O4 through holes that are consistently dispersed over a variety of nanosheets

## Slide 7: The conversion of Mn3O4 into MnO2 may be accomplished using a variety of chemical and electrochemical processes, and both are very helpful. For instance, the waste material Mn3O4 from batteries may be converted into MnO2, which would result in improved super capacitive characteristics The mix phases of manganese oxide (Mn3O4 and MnO2) may be easily regulated and manufactured by adjusting the amount of time that an acid treatment is given, and this can be done anytime it is necessary for any purpose.

## Slide 8: References
Pathan H, Lokhande C. Deposition of metal chalcogenide thin films by successive ionic layer adsorption and reaction (SILAR) method. Bulletin of Materials Science. 2004;27: 85-111
M. Saranya, R. Ramachandran, F. Wang, Graphene-zinc oxide (G-ZnO) nanocomposite for electrochemical supercapacitor applications, Journal of Science: Advanced Materials and Devices, 1 (2016) 454-460.
Y. Dai, K. Wang, J. Xie, From spinel Mn3O4 to layered nanoarchitectures using electrochemical cycling and the distinctive pseudocapacitive behavior, Applied Physics Letters, 90 (2007) 104102.

## Slide 9: 4. X. Liu, C. Chen, Y. Zhao, B. Jia, A review on the synthesis of manganese oxide nanomaterials and their applications on lithium-ion batteries, Journal of Nanomaterials, 2013 (2013). 5. X. Hao, J. Zhao, Y. Li, Y. Zhao, D. Ma, L. Li, Mild aqueous synthesis of octahedral Mn3O4 nanocrystals with varied oxidation states, Colloids and Surfaces A: Physicochemical and Engineering Aspects, 374 (2011) 42-47. 6. J.-Y. Li, H.-Y. Lü, X.-H. Zhang, Y.-M. Xing, G. Wang, H.-Y. Guan, X.-L. Wu, P2- type Na0.53MnO2 nanorods with superior rate capabilities as advanced cathode material for sodium ion batteries, Chemical Engineering Journal, 316 (2017) 499-505.

## Slide 10: Thank You