## Slide 1
Investigation into the Interplay of Structural, Electrical, and Magnetic Attributes in Al3+ Substituted Ni-Zn-Co Ferrites

## Slide 2
SUBHAJIT GHANA
SC19BPHDPH002
Enrollment No.
PHYSICS
Dr. SUDHAKAR SINGH
SARDAR PATEL UNIVERSITY, BALAGHAT

## Slide 3
This study explores the complex interactions between structural, electrical, and magnetic properties in Ni-Zn-Co ferrites replaced by Al3+. Ferrites' exceptional magnetic capabilities make them useful in a wide range of technological applications. The ferrite lattice's structural, electrical, and magnetic properties are significantly altered when Al3+ ions are added as replacements. Although research in this field is still in its early stages, this work investigated the structural, electrical, and magnetic properties of diamagnetic aluminium (Al3+) substituted nickel-zinc-cobalt (Ni–Zn–Co) mixed spinel ferrites. The space group Fd3m, which denotes the crystallinity of the particle, was used to index selected area electron diffraction (SAED) patterns.

## Slide 4
The range of the optical band gaps was 6.786 eV to 6.768 eV. Measurements of ac conductivity and frequency-dependent dielectric constants indicated that the produced ferrites were extremely resistant. With composition x, relaxation times decreased to a low value of 2.56 ms from 47.47 ms. For every sample, the Curie temperatures (Tc) ranged from 617 to 625 K. With relative quality factors (RQF) of about 105, real part permeabilities (m/) were comparatively steady up to an extended frequency range of 108 Hz. Adjusting the characteristics suggests that the produced ferrites could have potential use in high-frequency electronic gadgets. This study advances our understanding of ferrite materials and offers suggestions for improving them in real-world uses.