## Slide 1
Abdul Jabbar, Dr. Kishan Pal Singh
Department of Mechanical Engineering
Mangalayatan University, Aligarh
Analysis of Process Parameters and its Influence in Additive Manufacturing

## Slide 2: Presentation Outline
Introduction
Materials and Methods
3D Acquisition and CAD Modelling
Dimensional Inspection
Circularity and Cylindricity Control
Conclusions
References

## Slide 3: Introduction
All of the methods that allow for the successive addition of extremely thin material layers to create three-dimensional objects are collectively referred to as additive manufacturing, or AM.
The first generation of additive manufacturing (AM) systems were restricted to industrial uses due to the progress of additive technology.
However, due to their remarkable level of innovation, AM systems are now widely used.
These days, a broad spectrum of users—many of whom are not engineering experts—commonly use the words additive manufacturing and 3D printing.
In fact, the widespread availability of inexpensive 3D printers has made it possible for regular consumers to utilize this technology, allowing them to quickly and more affordably create 3D objects at home.

## Slide 4: Materials and Methods
A Da Vinci 1.0A 3D printer was used to build the prototypes that are being considered.
The Da Vinci 1.0A is powered by the exclusive "XYZware" software, and it can construct up to 20x20x20 cm with compatibility for both PLA and ABS filaments.
Regretfully, you are unable to accurately and individually alter the printing parameters using this software. For this, the programs "Slic3r" and "Simplify3D" were utilized.
To start the printing process, the ".gcode" files produced by these programs—which included the mandated set of printing parameters—were loaded into the XYZware program

## Slide 5: 3D Acquisition and CAD Modelling
A typical reverse engineering method was used to check the printed components for dimensions and shape accuracy .
Using a 3D laser scanner based on triangulation, Hexagon metrology was able to obtain all of the prototypes .
This device can acquire point clouds at a high rate (150000 points per second) with a high degree of accuracy (0.013 mm) and has programmable line lengths.
After post-processing and conversion into NURBS surfaces, the obtained point clouds produced models that deviated from the point clouds by less than 0.035 mm
The last stage of the procedure was turning the NURBS surfaces into CAD solid models.
Each prototype CAD model has been successively aligned with the nominal CAD model.

## Slide 6: Dimensional Inspection
The deviation values, which were defined as the shortest path between any point on the nominal CAD model and the obtained model, were measured in order to perform the dimensional inspection.
To obtain data regarding the printed object's dimensional accuracy, Root Mean Square Errors (RMSE) have also been computed.
Colored maps that represent the distributions of deviation values throughout the CAD models of the prototypes are shown in Figure 7.
These maps demonstrate that the z-axis is where the biggest discrepancies between the nominal CAD model and the obtained models occur.
The prototypes are really all smaller than the nominal cylinder.

## Slide 7: Conclusions
This paper presents the results of a study on the impact of certain parameters of AM processes.
A thorough investigation was carried out to evaluate the dimensions and geometric accuracy of a cheap 3D printer.
In specifically, different levels of layer thickness have been printed on a few cylindrical specimens. Using a conventional reverse engineering method, these prototypes were acquired and transformed into CAD models.
Then, by comparing these models to the nominal CAD model, the maximum deviation values and root mean square errors were computed. Additionally, controls for cylinder and circularity were performed

## Slide 8: References
  Bikas,H., Stavropoulos, P., Chryssolouris, G., Additive manufacturing methods and modeling approaches: A critical review, 2016, International Journal of Advanced Manufacturing Technology,83(1-4),pp.389-405
  Guo,N., Leu, M.C., Additive Manufacturing: Technology, applications and research heeds,2013,Frontiers of Mechanical Engineering,8(3),pp.215-243
  Lanzotti, A., DelGiudice, D.M., Lepore, A.,Staiano, G.,Martorelli, M., on the geometric accuracy of Rep Rap open-source three-dimensional printer, 2015, Journal of Mechanical Design, Transactions of theASME,137 (10),art.no.101703
  Cerniglia, D.,Montinaro, N.,Nigrelli, V.,Detection of disbands in multi-layers tructures by laser-based ultra sonic technique,2008, Journal of Adhesion, 84(10),pp.811-829
  Boschetto, A.,Bottini,L. Accuracy prediction in fused deposition modelling, 2014, International Journal of Advanced Manufacturing Technology, 73 (5-8), pp.913-928
  Ingrassia,T., Mancuso,A., Nigrelli,V., Tumino, D., Numerical study of the components positioning influence on the stability of a reverse shoulder prosthesis (2014) International Journal on Interactive Design and Manufacturing, 8(3), pp.187-197