## Slide 1: EXPERIMENTAL STUDY ON PARTIAL REPLACEMENT OF COARSE AGGREGATE WITH COCONUT SHELL
Tung Messar1, Talkeshwar Ray2
1Post Graduate Student, Department of Civil Engineering, Himalayan University, Itanagar Arunachal Pradesh, India
2Assistant Professor, Department of Civil Engineering, Himalayan University, Itanagar Arunachal Pradesh, India
Corresponding Author: Tung Messar

## Slide 2: introduction
Infrastructure development across the world created demands for construction material. In this constructed environment, the rising cost of building construction materials is the factor of great concern.
The cost of building materials are raising day by day. Now a days most of the researchers have focus on use of the waste materials in concrete according to their properties.
. Fly ash, Rice husk, Slag and Sludge from the treatment of industrial and domestic waste water has been found suitable as a replacement for cement in concrete.
The coconut shell is also a material used as a replacement for cement in concrete. In this work we are partially replacing the coarse aggregate with coconut shell.

## Slide 3: LITERATURE REVIEW
B. Damodhara Reddy and colleagues (2014) Presented in this study are the physical and chemical characteristics of coconut shell and coconut shell aggregate concrete, as well as the feasibility of using coconut shell aggregate in construction. When compared to conventional aggregate, the moisture content and water absorption were 4.20 percent and 24 percent, respectively. These values are higher than those of conventional aggregates. When crushed, the density of the coconut shell may be as high as 550-650 kg/m3, which is well within the boundaries of what, is required for light weight aggregate.

## Slide 4
Daniel Yaw Osei and colleagues (2013) According to the findings of his publication, there is potential for the use of coconut shell as a replacement for conventional aggregate in both conventional reinforced concrete and light-weight reinforced concrete. Coconut shell concrete aids in the protection of natural resources.
Yogesh Narayan Sonawane and colleagues (2016) In their diary, they talked about a variety of different topics. It has been discovered that coconut shell concrete offers greater workability due to the smooth surface on one side of the shell, which was discovered during the research. As long as the sugar is not in a free sugar form, the presence of sugar in the CS will have no effect on the setting strength of concrete. The shell does not disintegrate quickly due to the strong tissue that it is formed of, and it stays as a solid waste for many years.

## Slide 5: MIX DESIGN FOR M20 GRADE OF CONCRETE
Step 1: Stipulation for proportioning
a) Grade designation : M20
b) Types of cement : PPC 53 grade
c) Maximum nominal size of coarse aggregate : 20mm
d) Minimum water content : 345kg/m3 (As per IS: 456-2000)
e) Maximum water cement ratio : 0.5 (As per IS: 456-2000 Table 5)

## Slide 6
Step 2: Test data for materials
a) Cement used : PPC 53 grade
b) Specific gravity of cement : 2.5
c) Specific gravity of
Coarse aggregate : 2.87
Fine aggregate : 2.67
Step 3: Determination of target strength
Standard deviation (σ) for M20 IS 4.0 taken as per IS-10262- 2019 Target Strength = fck + 1.65 ×σ
                = 20 + 1.65 × 4.0
                = 26.6 N/mm2

## Slide 7
Step 4: Selection of water-cement ratio
Adopt water-cement ratio = 0.5
Step 5: Water content
For 20mm nominal maximum size of aggregate, water content per cubic meter of concrete = 186L
Step 6: Selection of cement content
Water cement ratio = 0.5 Cement content = 186/0.5
= 372 Kg/m3

## Slide 8
Step 7: Volume of Coarse aggregate and Fine aggregate
As per IS 10262-2009 Table No.3 Volume of coarse aggregate = 0.62m3
Volume of fine aggregate = (1-volume of C.A)
= 1-0.62
= 0.38m3
Step 8: Mix Calculation
Volume of concrete = 1m3
Volume of cement = mass of cement/specific gravity × 1000
= (372/2.5) × (1/1000)
= 0.1488m3

## Slide 9
Volume of water = mass of water/specific gravity of water×1000
= (186/1) × (1/1000)
= 0.186m3
Volume of all in aggregate = 1-(0.1488+0.186)
= 0.66m3
Coarse aggregate =0.66×0.62×2.87×1000
= 1174.404Kg/m3
Fine aggregate = 0.66×0.38×2.67×1000
= 669.636Kg/m3

## Slide 10: RESULTS AND CONCLUSION
The compression test is widely regarded as the most common test conducted on hardened concrete due to its direct correlation with many desirable characteristic properties. This test is crucial because the compressive strength of concrete serves as a fundamental indicator of its overall quality and performance in structural applications.
During the compression test, specimens in the form of cubes are subjected to increasing compressive loads until failure occurs. These cube specimens typically have dimensions of 150×150×150 mm, adhering to standard testing protocols. The size and shape of the cubes allow for uniform loading and accurate measurement of compressive strength.

## Slide 11
Compressive strength, measured in megapascals (MPa) or pounds per square inch (psi), represents the maximum load-bearing capacity of concrete under axial compression. It indicates the ability of concrete to withstand applied loads and resist deformation or failure. Various factors, including the quality of materials, mix proportions, curing conditions, and age of concrete, influence the compressive strength.
The results of compression tests provide valuable insights into the structural integrity, durability, and serviceability of concrete elements, such as beams, columns, slabs, and foundations. Engineers use these test results to assess the suitability of concrete mixes for specific design requirements, verify compliance with industry standards and specifications, and ensure the safety and reliability of constructed structures.
In short, the compression test on concrete cube specimens serves as a critical quality control measure, offering quantitative data on compressive strength and guiding engineering decisions throughout the design, construction, and maintenance phases of infrastructure projects.

## Slide 12
S.N0 | Specimens | Coarse aggregate (kg) | Coconut shell(g) | Date of casting | Date of testing | Weight of cube | Load (KN) | Compressive strength
1 | M1 | 3.9 | 100 | 14/05/24 | 20/05/24 | 7252 | 320 | 14.22
2 | M1 | 3.9 | 200 | 14/05/24 | 20/05/24 | 7310 | 360 | 16.00
3 | M1 | 3.9 | 300 | 14/05/24 | 20/05/24 | 7289 | 350 | 15.55
Table 1: Compressive strength of concrete replaced with coconut shell at 7 days

## Slide 13
S.N0 | Specimens | Coarse aggregate (kg) | Coconut shell(g) | Date of casting | Date of testing | Weight of cube | Load (KN) | Compressive strength
1 | M2 | 3.8 | 100 | 14/05/24 | 27/05/24 | 7440 | 420 | 18.66
2 | M2 | 3.8 | 200 | 14/05/24 | 27/05/24 | 790 | 450 | 20.00
3 | M2 | 3.8 | 300 | 14/05/24 | 27/05/24 | 7435 | 410 | 18.22
S.N0 | Specimens | Coarse aggregate (kg) | Coconut shell(g) | Date of casting | Date of testing | Weight of cube | Load (KN) | Compressive strength
1 | M3 | 3.7 | 100 | 14/05/24 | 10/06/24 | 8149 | 510 | 22.66
2 | M3 | 3.7 | 200 | 14/05/24 | 10/06/24 | 8477 | 540 | 24.00
3 | M3 | 3.7 | 300 | 14/05/24 | 10/06/24 | 8412 | 520 | 23.11
Table 3: Compressive strength of concrete replaced with coconut shell at 28 days
Table 2: Compressive strength of concrete replaced with coconut shell at 14 days

## Slide 14: REFERENCES
Amarnath Yerramala Ramachandrudu C, Properties of Concrete with Coconut Shells as Aggregate Replacement, International Journal of Engineering Inventions, vol.1, Issue 6, October 2012.
A short and W.Kinniburgh, Lightweight Concrete, Applied Science Publishers, London
Adeyemi AY.,(1998) ,“ An investigation into the suitability of coconut shells as aggregates in concrete production” ,Journal of Environment, Design and Management.
J. P. Ries, J. Speck, (2010), “Lightweight Aggregate Optimizes the Sustainability of Concrete”, Concrete Sustainability Conference, National Ready Mixed Concrete Association.
J.M.Crow, The Concrete Conundrum, 2006, available at www.chemistryworld.com

## Slide 15
THANK YOU