## Slide 1: EXPLORING ALBUMIN MICROSPHERES FOR ENHANCED DELIVERY OF KETOPROFEN: FORMULATION AND ASSESSMENT
1Bikram Kumar Sahu*, 2Gourav Sahu, 3Kalpana Mahapatra, 4Sarmistha Das, 5Rashika Shrivastav, 6Sarthak Behera, 7Dibyajyoti Pani
Roland Institute of Pharmaceutical Sciences, Brahmapur, Odisha

## Slide 2
INTRODUCTION
Microspheres are defined as small, solid, spherical particles ranging from 1 to 1000 μm in diameter, made from a variety of polymeric, waxy, or protective materials.
These materials may include synthetic biodegradable polymers, such as polylactic acid and polyglycolic acid, and modified natural products, including starches, gums, proteins, fats, and waxes. Natural polymers, like albumin and gelatin, offer advantages as they are derived from living organisms, are readily available, cost-effective, eco-friendly, and can undergo various chemical modifications.
Microspheres possess a high surface-to-volume ratio, making them ideal for applications in drug delivery systems due to their colloidal properties and enhanced interfacial activity. In recent years, microspheres have gained significant attention for their potential to improve drug stability, enhance handling, and deliver drugs in a controlled, sustained-release manner.
The pharmaceutical industry has explored microspheres for diverse applications such as converting oils and liquids into solids, taste masking, improving drug stability, and enhancing flow properties of powders.

## Slide 3
A sustained-release form, particularly using albumin microspheres, has the potential to alleviate these issues, improve patient compliance, and reduce adverse effects.
Albumin, which constitutes a significant portion of plasma proteins, has shown promising results in sustained-release systems and as a carrier for tumor-targeted therapies due to its selective accumulation in solid tumors. Research has highlighted its utility in targeting drugs to inflamed joints in rheumatoid arthritis, as albumin binds to the synovium similarly to tumor cells, thereby increasing drug circulation half-life and minimizing distribution to non-target tissues.
This specificity reduces adverse effects and improves treatment efficiency, demonstrating albumin’s versatility in biomedical applications.
Various techniques for preparing albumin microspheres include solvent evaporation, spray drying, wax coating, coacervation, and chemical cross-linking.
Each technique offers distinct benefits based on parameters such as particle size, drug encapsulation efficiency, and desired release profile. For example, solvent evaporation is suitable for both aqueous and non-aqueous systems, making it a flexible option, while spray drying provides a rapid and single-step approach for heat-sensitive materials.

## Slide 4
LITRETURE REVIEW
Murali Mohan Babu GV et al. formulated a controlled-release version of Diclofenac Sodium using a gum karaya-chitosan complex via the coacervation method. In vivo studies revealed a sustained blood level pattern for the microcapsules, comparable to that of a commercial controlled-release formulation, highlighting the potential for extended drug action through natural polymer complexes.
Thakkar H et al. prepared Celecoxib-loaded albumin microspheres using BSA through an emulsification chemical cross-linking method. In vitro release studies indicated that the microspheres could sustain drug release for approximately six days. Blood kinetic studies further revealed that Celecoxib-loaded albumin microspheres provided prolonged circulation compared to a standard Celecoxib solution.
Rajamanickam D et al. formulated albumin microspheres containing Aceclofenac aimed at providing sustained release. Egg albumin was employed as a release-retarding agent, resulting in discrete, spherical microspheres with an average particle size of 99.6 μm. The optimized formulation exhibited significant analgesic and anti-inflammatory activity, underlining the utility of albumin microspheres as effective release-retarding agents.

## Slide 5
RESEARCH METHODOLOGY
Bovine serum albumin microspheres were prepared using a solvent evaporation method, adapted from Tabassi et al. with slight modifications.
A 1% w/v solution of BSA was prepared in distilled water, and Ketoprofen (KP) was dispersed into this solution. This mixture was then dispersed in 100 ml of sunflower oil containing 0.5 ml of Tween 80 in a 200 ml beaker, and stirred at 600 rpm for 30 minutes.
After stirring, the microspheres were centrifuged, washed several times with petroleum ether and acetone, then dried at 50°C, and stored in a desiccator.
Evaluation of Ketoprofen-Loaded Albumin Microspheres
1. Drug-Polymer Interaction (FTIR) Study
FTIR spectroscopy was performed on a Fourier transform infrared spectrophotometer (IR Affinity-1, Shimadzu, Japan). Drug and potassium bromide pellets were prepared by compressing the powders at 20 psi for 10 minutes on a KBr press, and

## Slide 6
spectra were scanned in the wave number range of 4000-600 cm⁻¹. FTIR analysis was conducted on KP, a physical mixture of KP and polymer, KP microspheres, and blank microspheres.
Surface Morphology (SEM)
Scanning electron microscopy (SEM) was used to determine particle size distribution, surface topography, and morphology. SEM analysis was conducted using a JEOL JSM T-330A scanning microscope (Japan). Dry KP microspheres were placed on a brass stub, coated with an ion sputter, and imaged by random scanning.
Frequency Distribution Analysis
The average particle size of KP microspheres was measured using optical microscopy with a stage micrometer. A small amount of KP microspheres was spread on a clean glass slide, and the size of 300 microspheres was recorded for each batch. A histogram was created to present the particle size distribution.
Percentage Yield
The percentage yield was calculated to evaluate the efficiency of the production method, using the formula:
Percentage Yield=(Practical YieldTheoretical Yield)×100\text{Percentage Yield} = \left( \frac{\text{Practical Yield}}{\text{Theoretical Yield}} \right) \times 100Percentage Yield=(Theoretical YieldPractical Yield​)×100

## Slide 7
Practical Drug Content Analysis
KP microspheres equivalent to 100 mg of KP were dissolved in 100 ml of phosphate buffer (pH 7.0) and allowed to dissolve completely overnight. After filtering and diluting to a concentration of 10 µg/ml, absorbance was measured at 258 nm, and the percentage of KP was calculated.
In Vitro Dissolution Studies
Calibration Curve of Ketoprofen
The calibration curve of Ketoprofen in phosphate buffer (pH 7.0) was constructed as previously described.
Dissolution Studies
Dissolution studies were conducted using a USP XXIII dissolution apparatus in phosphate buffer (pH 7) for 12 hours, with a maintained temperature of 37 ± 0.5°C and a basket rotation speed of 50 rpm. Samples were withdrawn at 1-hour intervals and replaced with fresh dissolution media. The amount of KP released was measured by UV absorption at 258 nm.

## Slide 8
Kinetics of Drug Release
The in vitro release data were fitted to various kinetics models:
Cumulative Percentage Drug Release vs. Time (Zero Order)
Log Cumulative Percentage Drug Retained vs. Time (First Order)
Cumulative Percentage Drug Release vs. √T (Higuchi’s Model)
Log of Cumulative Percentage Drug Release vs. Log Time (Peppas Model)
Differential Scanning Calorimetry (DSC)
The physical state of KP in the microspheres was analyzed by Differential Scanning Calorimetry (Mettler-Toledo star 822e system, Switzerland), with thermograms recorded at a scanning rate of 10°C/min over a temperature range of 25–300°C.
X-Ray Power Diffractometry (XRD) Study
XRD analysis of KP, the KP-polymer physical mixture, and KP microspheres was performed using a Joel JDX-8030 diffractometer with graphite crystal monochromator (Cu-Kα) radiation to determine the physical state of KP in the microspheres.

## Slide 9
RESULT AND DISCUSSIONS
The present study reports a novel attempt to prepare microspheres of the non-steroidal anti-inflammatory drug (NSAID) Ketoprofen (KP) using a natural polymer, Bovine Serum Albumin (BSA), as a carrier for improved treatment of rheumatoid arthritis, pain, inflammation, and related conditions.
The microspheres of KP were prepared by the solvent evaporation method utilizing BSA. Various evaluation parameters were assessed with the aim of obtaining a sustained release of KP.
Preformulation Studies
The solubility of KP in 10 mg/10 ml of solvent was assessed, revealing that KP is freely soluble in ethanol, chloroform, acetone, and ether, and soluble in benzene and strong alkali, but practically insoluble in water at 20°C.
The melting point of KP was found to be 94°C, complying with IP standards, thus indicating the purity of the obtained drug sample. A solution of KP with a concentration of 10 µg/ml was prepared in ethanol, and the UV spectrum was taken using a Shimadzu (UV-1800) double beam spectrophotometer, scanning between 200 to 400 nm.

## Slide 10
Evaluation of Ketoprofen Microspheres
Drug-Polymer Interaction (FTIR) Study
Surface Morphology of Ketoprofen Microspheres (SEM)
Frequency Distribution Analysis
Percentage Yield
Percentage Drug Entrapment Efficiency
In Vitro Dissolution Studies
Release Kinetics of Ketoprofen Microspheres
Differential Scanning Calorimetry (DSC)
X-Ray Powder Diffractometry (XRD)
Figure 1: FTIR Spectrum of Ketoprofen microspheres using Bovine serum albumin of the optimized formulation

## Slide 11
Figure 2: SEM of Ketoprofen microspheres using Bovine serum albumin of the optimized formulation
Figure 3: XRD of Ketoprofen microspheres using Bovine serum albumin of the optimized formulation

## Slide 12
Formulation | Zeroorder | Firstorder | HiguchiMatrix | Peppasplot | 
 |  |  |  | r2value | ‘n’value
KP1 | 0.9927 | 0.9227 | 0.9758 | 0.9881 | 0.7082
KP2 | 0.9930 | 0.9512 | 0.9741 | 0.9868 | 0.7084
KP3 | 0.9959 | 0.9671 | 0.9764 | 0.9928 | 0.7634
KP4 | 0.9971 | 0.9773 | 0.9764 | 0.9937 | 0.7952
KP5 | 0.9990 | 0.9820 | 0.9761 | 0.9978 | 0.8705
KP6 | 0.9472 | 0.8867 | 0.8587 | 0.9162 | 0.8992
Table 1 : Regression co-efficient (r2) values of different kinetic models and diffusion exponent(n)of Peppas model for Ketoprofen microspheres

## Slide 13
CONCLUSION
Preformulation studies, including solubility, melting point, and UV analysis of ketoprofen (KP), complied with IP standards.
The FTIR spectra revealed no interaction between the polymers and KP, indicating compatibility of all the polymers used with KP. Surface smoothness of the KP microspheres increased with higher polymer concentration, as confirmed by SEM analysis.
Entrapment efficiency improved with an increase in polymer concentration.
The results suggest a proper distribution of KP within the microspheres, with deviations falling within acceptable limits.
The study further indicated that the amount of drug release decreased with increasing polymer concentration, demonstrating that the in vitro performance of KP microspheres showed prolonged and sustained release of the drug. The coefficient of determination indicated that the release data were best fitted with zero-order kinetics.
The Higuchi equation explains the diffusion-controlled release mechanism, while the diffusion exponent ‘n’ values from the Korsmeyer-Peppas model ranged from 0.5 to 1, indicating Non-Fickian drug transport through the KP microspheres prepared with BSA. DSC and XRD data indicated that KP remained in its lattice structure in the physical mixture, while it was completely amorphous inside the KP microspheres.

## Slide 14
REFERENCES
Remington. The science and practice of pharmacy. 21st ed. Vol. 1. Philadelphia, PA: Lippincott Williams and Wilkins; 2005. p. 939.
Avera. Available from: http://www.pharmaceutical-technology.com/contractors/drug_delivery/avera/avera2.html. Nov 2010.
Eroglu H, Suheyla KASH, Oner L, Sargon M, Hincal AA. Preparation of bovine serum albumin microspheres containing Dexamethasone Sodium Phosphate and the in vitro evaluation. Turk J Med Sci. 2000;30:125–8.
Hong W, Kinam P. Oral controlled formulation design and drug delivery: Theory to practice. 1st ed. 6.
Venkatesan P, Manavalan R, Valliappan K. Microencapsulation: a vital technique in novel drug delivery system. J Pharm Sci & Res. 2009;1(4):26-35.
Gunja C, Prakash B, Saha RN. Microspheres technology and its applications. Nov 2010.
Jain NK. Biodegradable polymers: Controlled and Novel Drug Delivery. 1st ed. p. 81-239.
Murali Mohan Babu GV, Himasankar K, Churuvu PS, Narayan R, Ramana Murthy KV. Controlled release of diclofenac sodium by gum karaya-chitosan complex coacervate: In vivo evaluation. Indian J Pharm Sci. 2001;63(5):408-12.

## Slide 15
THANK YOU